## Slide 1
Levard et al.
Goethite, a tailor-made host for the critical metal scandium: The FexSc(1-x)OOH solid solution
Levard et al. (2018) Geochem. Persp. Let. 9, 16-20 | doi: 10.7185/geochemlet.1832
© 2018 The Authors
Published by the European Association of Geochemistry
under Creative Commons License CC BY-NC-ND.
Figure 2 Top: Changes in cell parameters and in cell volume as a function of rate of substitution of Fe by Sc (numerical data for cell parameters and errors can be found in SI). Dashed lines represent ideal Vegard’s law behaviour. Bottom: Crystal structure of goethite. The octahedrons represent the Fe surrounded by 6 oxygen atoms. Spheres represent the hydrogen atoms.
Notes: Figure 2 Top: Changes in cell parameters and in cell volume as a function of rate of substitution of Fe by Sc (numerical data for cell parameters and errors can be found in SI). Dashed lines represent ideal Vegard’s law behaviour. Bottom: Crystal structure of goethite. The octahedrons represent the Fe surrounded by 6 oxygen atoms. Spheres represent the hydrogen atoms.
Figure 1 (a) Structure factors, S(q), of molten CaCO3; curves are stacked to see better the evolution with increased P-T conditions (given on the right panel); the main change affecting S(q) (Fig. 1a) is the shift of the first sharp diffraction peak (FSDP) towards higher reciprocal distances, up to 2.28 Å-1 at 8.7 GPa which corresponds in the real space to a characteristic mid-range order distance, 2𝜋/𝑞_𝐹𝑆𝐷𝑃, of 2.76 Å. (b) Corresponding radial distribution functions (plain curves), g(r), compared to MD simulations (dashed curve; Vuilleumier et al., 2014).